**0W-30 SN / CF DPF**

0W-30 is a blend of advanced technology components formulated to be fully compatible with the latest Diesel Particulate Filters (DPFs) and Gasoline Catalytic Converters (CATs). The 0W-30 is designed to help provide superior performance and protection with potential fuel-saving benefits.

**Certificates And Standards:**

API SN ; API SL, API CF,

ACEA C2, ACEA C3,

MB-Approval 229.31, MB-Approval 229.51, MB-Approval 229.52,

Porsche C30, VW 504 00

***Technical Specifications***

|  |  |  |
| --- | --- | --- |
| **Test** | **Method** | **Typical Properties** |
| **Kinematic Viscosity (100°C), [cSt]** | ASTM D445 | 9,3-12,5 |
| **Viscosity Index** | ASTM D2270 | Min. 150 |
| **Flash Point, °C** | ASTM D92 | Min. 220 |
| **Pour Point, °C** | ASTM D97 | Max. -40 |