**20W-50 CF-4/SJ**

20W-50, is an engine oil that can be used in any kind of modern and old diesel engines during the whole year. It is suitable to be used in fleets including lorry kinds having high motor powers so as to carry heavy loads. The special combination of high quality base oil with state-of-art additive technology provides effective protection and lubrication during the usage period of this oil.

**Certificates And Standards:**

 API CF-4/SJ,

ACEA E2,

Allison C4,

MB 227.1,

CAT TO-2,

MIL-L 2104 B

***Technical Specifications***

|  |  |  |
| --- | --- | --- |
| **Test** | **Method** | **Typical Properties** |
| **Appearance** | Visual | Clear-Bright |
| **Kinematic Viscosity (100°C), [cSt]** | ASTM D445 | 16,3-21,9 |
| **Viscosity Index** | ASTM D2270 | Min. 120 |
| **Flash Point, °C** | ASTM D92 | Min. 225 |
| **Pour Point, °C** | ASTM D97 | Max. -21 |
|  |  |  |