**HD SERIES CC/SC**

Is monograde engine oil that is intended for general usage in any kind of passenger, normal suction or turbo charge commercial diesel engine. Monograde motor oils are not suitable to be used for the whole year, therefore, appropriate SAE level product should be chosen in accordance with season and temperature conditions. It is recommended to be used in passenger and commercial vehicles and heavy duty diesel vehicles.

**Certificates And Standards:**

API CC/SC

***Technical Specifications***

|  |  |  |
| --- | --- | --- |
| **Test** | **Method** | **Typical Properties** |
|  |  **10 30**  |  **30 40 50 60** |
| **Appearance** | Visual |  Clear & Bright |
| **Kinematic Viscosity (100°C), [cSt]** | ASTM D445 4,5-6,5  |  9,3-12,5 12,5-16,3 16,3-21,9 21,9-26,1  |
| **Viscosity Index** | ASTM D2270 min. 100 |  min. 90 min.90 min.90 min.90  |
| **Flash Point, °C** | ASTM D92 min. 185 |  min. 220 min.220 min.220 min.220  |
| **Pour Point, °C** | ASTM D97 max. -24 | max. -15 max.-15 max.-15 max.-10  |
|  |  |  |