**BENTONITE GREASE**

It is a bentonite thickener grease that provides superior performance at very high temperatures. In low-speed and high-temperature plain bearings, plain and roller bearings; in central automatic lubrication systems; It is used in industrial applications such as marble, brick, oven, road, construction, glass. Bentonite grease in heavy load and shock impact systems; It is suitable for use in high temperature and open gear systems.

***Technical Specifications***

|  |  |  |
| --- | --- | --- |
| **Test** | **Method NLGI 1 NLGI 2 NLGI 3**  |  |
| **Color** |  Yellow or Brown |  |
| **Soap Type** | ASTM D2270 Bentonite  |  |
| **Cone Penetration, worked, 0,1 mm, 25 °C /**  | ASTM D217 310-340 265-295 220-250 |  |
| **Dropping Point, °C** | ASTM D566 min 300 min 300 min 300 |  |