**LITHIUM EP GREASE**

LITHIUM EP GREASE, it is an automotive grease formulated with high quality mineral base oils, specially selected additives (EP), and another additive for extreme pressures. It is recommended for industrial applications under heavy duty and impact conditions, and for wheel bearings and central lubrication systems of automobiles, commercial vehicle, sports utility vehicles, agricultural machines, and heavy duty machines. It’s safely used at operating temperature not exceeding 180 °C.

***Technical Specifications***

|  |  |  |
| --- | --- | --- |
| **Test** | **Method NLGI 00 NLGI 0 NLGI 1 NLGI 2 NLGI 3** |  |
| **Color** | Yellow Brown |  |
| **Soap Type** | ASTM D2270 Lithium |  |
| **Cone Penetration, worked, 0,1 mm, 25 °C /** | ASTM D217 400-430 355-385 310-340 265-295 220-250 |  |
| **Dropping Point, °C** | ASTM D566 min 185 min 185 min 185 min 185 min 185 |  |