**GEAR BOXES**

GEAR BOXES are high performance gear oils that are formulated for closed system gears, reinforced with extreme pressure (EP) and special additives, working under extreme load and pressure. They show high performance for a long time without deteriorating their chemical and thermal stability at operating temperatures between -15 °C and 120 °C (according to their viscosity values).

**Certificates And Standards:**

David Brown S1.53.101 (E), USS 224, AGMA 9005-E02, DIN 51517 Part 3

***Technical Specifications***

|  |  |  |
| --- | --- | --- |
| **Test** | **Method** | **68 100 150 220 320 460 680** |
| **Kinematic Viscosity (40°C), [cSt]** | **ASTM D445** | **61,2- 90- 135- 198- 288- 414- 612-**  **74,8 110 165 242 352 506 748** |
| **Viscosity Index ,min** | ASTM D2270 | 90 90 90 90 90 90 85 |
| **Flash Point ,min °C** | ASTM D92 | 180 200 200 200 200 200 200 |
| **Pour Point ,max °C** | ASTM D97 | -12 -12 -9 -9 -9 -9 -9 |