**LIGHT MACHINE OIL**

It is a special oil that is formulated by using well refined base oils. It has a wide range of applications in industry as a multi-purpose lubricator. It is successfully used in applications such as systems requiring thin oil and in air conditioners

***Technical Specifications***

|  |  |  |
| --- | --- | --- |
| **Test** | **Method** | **Typical Properties** |
| **Appearance** | Visual | Clear &Bright |
| **Kinematic Viscosity (40°C), [cSt]** | ASTM D445 | 15 |
| **Viscosity Index** | ASTM D2270 | Min. 95 |
| **Flash Point, °C** | ASTM D92 | Min. 200 |
| **Pour Point, °C** | ASTM D97 | Max. -12 |
|  |  |  |