**MOULD OIL 32**

MOULD OIL, is a qualified oil formulated from quality base oils obtained through modern refining processes. It has been developed for the construction industry to prevent concrete from sticking to the moulds. It is recommended to be used in steel and wooden molds with its composition containing quality base oils and special additives.

***Technical Specifications:32***

|  |  |  |
| --- | --- | --- |
| **Test** | **Method** | **Typical Properties** |
| **Appearance** | Visual | Clear &Bright |
| **Kinematic Viscosity (40°C), [cSt]** | ASTM D445 | 15 |
| **Viscosity Index** | ASTM D2270 | Min. 95 |
| **Flash Point, °C** | ASTM D92 | Min. 100 |
| **Pour Point, °C** | ASTM D97 | Max. -6 |
|  |  |  |